Springfield Technical Community College

ACADEMIC AFFAIRS

| Course Number: | MECH 390 | Department: | MET |
| --- | --- | --- | --- |
| Course Title: | Materials and Processing for World-Class Manufacturing | Semester: | Fall | Year: | 2004 |

Objectives/Competencies

| Course Objective | Competencies |
| --- | --- |
| Understand and identify commonly used engineering materials. | Define the four classifications of materials: Metals, Polymers, Ceramics, and Composites. Compare and contrast the mechanical and physical properties of the different classifications of materials Define and visualize a BCC, FCC, and HCP unit cell Compare the density and relative strength between BCC, FCC, and HCP crystal structures |
| Understand the behavior and manufacturing properties of metals, plastics, ceramics and composites. | Visualize mechanical properties of a metal Calculate stress as =Force/Area Calculate strain as =L/L Generate a Stress-Strain Diagram from supplied Test Data Identify different points on the curve of the Stress-Strain Diagram Calculate Modulus of Elasticity as E=/ in the Elastic Region of the Stress-Strain Diagram Identify the physical properties that change given different heat treatment applications. Identify Quenching Identify Annealing Identify Martensite formation Identify Tempering Determine the correct method of quenching for a given engineering requirement. The student will determine the method using the Jominy End Quench method. Introduce the concepts and vocabulary of “polymers” with simple models |
| Understand why various manufacturing processes are used, and the advantages of the different processes. | Understand the terminology of casting processes, forming and shaping processes, and joining processes. Define Extrusion, Injection Molding, Compression and Transfer Molding, Blow Molding, Thermoforming, Powder Metallurgy Define green sand, plaster, investment casting, expanded polystyrene, die casting, and centrifugal casting as expendable or permanent casting methods Define Bulk deformation processes as Rolling, Forging, Extrusion, or Drawing. Define Sheetmetal processes as Bending, Drawing, or Shearing Define the various joining processes in manufacturing Define the elements that make up the manufacturing costs for a plastic injection molded part: part material cost, equipment operating cost, and tooling cost. Define the elements that drive tooling costs for an injection-molded part: part geometry, mold closure direction, and parting surface location. Visualize how the effects of changing part geometry, mold closure direction, and parting line selection can affect tooling costs. |